Cements – All Ceramic Restorations

Dual/self core resin cements should be used to optimise long term function and biocompatibility. Lifelike recommend Rely X Unicem from 3m ESPE.

Rely X is indicated for all types of ceramic restorations and has excellent marginal integrity and biocompatibility.

Contra-indicated Cements

Resin modified cements are contradicted for bonding ceramic restorations. These cements contain HEMA resin which is hydrophilic and can result in post-set expansion which may lead to a delayed fracture. Cements that are not compatible with all ceramic restorations are:-

- Fuji plus

- Rely X Luting

- Dyract-cem

- Embrace